Composite Battery Box design discussion
 To fit Mike W's Porsche 944
Former FVEAA Club Car

---
High level requirements
- What they have to hold
- To fit in to existing battery support structure
- Better, lighter, faster than steel
- Insulating properties desirable
- Environmental, flying rocks and road salt
- Design to increase probability of successful build by mere mortals (Mike and Jeff)
- Money is always a factor

---
What they have to hold
- Batteries! (If you are surprised you are probably in the wrong meeting)
- Two rear boxes each holding 20 cells 150 lbs
  - 13" x 27" x 10"
- One front box holding 14 cells 105 lbs
  - 13” x 20” x 10”
- I don't know which cells he has purchased or why. Feel free to grill him after the meeting.

---
Where they have to fit
Front Box
- Front box has the widest span unsupported.
- Edges, especially sharp ones, need to be managed to prevent wear.
- Design to attach and reduce movement.

---
Where they have to fit
Back Boxes
- Offered to mold in place integrating the structure to the box
- With the full frame the loads are lower than I was initially thinking
- Prevent movement

---
How do composites work
- At a high level this is similar to using an I-Beam
- The core (web) has to prevent the two layers (flanges) from getting closer together
- If it doesn't the bottom won't be put in tension and other bad things happen

---
Core material
- Multiple considerations for core material
  - Wood
  - Aluminum Honeycomb
  - Eurethane (two part expansion foam)
  - Polystyrene (pink or blue foam boards at Menards)
- Key features
  - High crush resistance while being light
  - Easy to form
  - Can the other materials stick to it
  - Readily available

---
Fabric reinforcement
- Provides the Tensile and Compressive strength to the panel
- Ideally non conductive and resistant to impact
- Three options readily available
  - S2 Fiberglass
  - Carbon Fiber
  - Kevlar
- Final decision not yet made, I prefer Kevlar or equivalent aramid fiber for this application
- Can be assembled from any combination

---
Resin
(stuff that makes the fabric hard)
- The resin adheres the fibers to each other and in this design the fabric to the core
- For mere mortals long working time (pot life) is desirable
- Prefer it to be less toxic and easy to work with
- Resistant to the automotive environment
- Epoxy is the clear choice and the one I have the most experience with
- We will be doing “wet layup” as we will apply liquid epoxy to dry cloth on the finished product

---
Design
- We don't want the batteries falling out on the ground
- The bottom is critical the sides are there for protection, insulation, and additional rigidity
- Could be different materials to save weight
- Completely cover the bottom first
- Build the sides and attach them to the bottom
- Maximizes the fabric on the bottom panel in critical areas.
- Best chance of the bottom being made perfectly

---
Weight
- Each back box foam should weigh 1.68 lbs
- The front box foam should weigh 1.33 lbs
- Each back box fabric should weigh 11 ounces
- The front box fabric should weigh 8 ounces
- Assuming the worst case I will double the fabric weight as an allowance for Epoxy
- Total weight of all three boxes combined should be about 8.5 lbs
- Same boxes in 16 gauge steel about 60 pounds

---
Money is always a factor
- Epoxy 1.5 gallons (lots) $75.50
- Foam for 4' x 8' sheet each $10.98
  - Steel boxes would require foam insulation anyway
- Assuming the most expensive, Kevlar at 60 inches wide, we would need 5 yards at $25 a yard for $125
- Mike will have to feed me $$$
- Should be done for around $300
- I don't know what it costs to have 3 steel boxes made? Audience participation!

---
Links
- Foam
  - http://www.uscomposites.com/foam.html
  - http://building.dow.com/na/en/products/insulation/supertuffr.htm
- I-Beam physics
- https://www.dlsweb.rmit.edu.au/toolbox/buildright/content/bcgbc4010a/04_struct_members/01_beams/page_004.htm
- Fabric reinforcement
- http://www.bgf.com/pages/data_sheet_detail/?fabric=1166&format=English
- specs on the 8.9 oz Satin weaze S Glass $13.95 per yard 38 inches wide
- Carbon Fiber the 5.7 oz x 42 inch wide $16 or 60 inch wide $21.50 with kevlar tracer
- http://www.bgf.com/pages/data_sheet_detail/?fabric=1127&format=English
- On the Kevlar front the 5 oz has the above specs. At $16.5 for 38 inches or $25 for 60 inches it is certainly in the running.
  - http://www.uscomposites.com/kevlar.html